## Slide 1
Quality Standards
Nitrile Safety Manufacturing Standards
TECHNICAL DATA SHEET
Features
Size | Reorder#
X-Small | 1210-5
Small | 1210-6
Medium | 1210-7
Large | 1210-8
X-Large | 1210-9
2X-Large | 1210-0
All specifications are subject to change without notice.
Specification (mm) |  |  |  |  | 
Size | Glove Length | Palm Width | Cuff Thickness | Palm Thickness | Finger Thickness
X-Small | 300 | 75 | 0.13 | 0.20 | 0.26
Small | 300 | 85 | 0.13 | 0.20 | 0.26
Medium | 300 | 95 | 0.13 | 0.20 | 0.26
Large | 300 | 105 | 0.13 | 0.20 | 0.26
X-Large | 300 | 115 | 0.13 | 0.20 | 0.26
2X-Large | 300 | 125 | 0.13 | 0.20 | 0.26
Handplus® Nitrile Safety Synthetic Gloves
©2019, , All Rights Reserved.
Physical Properties
Property | ASTM Minimum | Nitrile Safety®
 | Before Aging | Before Aging
Tensile (MPa) | 14 | 18
Elongation (%) | 500 | 500
 | After Aging | After Aging
Tensile (MPa) | 14 | 18
Elongation (%) | 500 | 500
Safety Sealed Packaging (S-XL) 50 Gloves/Box, 10 Boxes/Case | Safety Sealed Packaging (XXL) 45 Gloves/Box, 10 Boxes/Case
Soft Nitrile with Easy Donning Feature | 
Blue Color | 
10 mil thickness, 12-inch cuff | 
Superior puncture resistance | 
Exceptional strength and durability | 
Textured finish for excellent grip | 
Better chemical barriers than latex gloves | 
Excellent tactile sensitivity and comfortable fit | 
Dated Lot Codes for quality assurance and traceability | 
Testing Methods
Meets or exceeds the following standards: ASTM D6319 (USA), EN 455 (EEC), A5 40 (AUSTRALIA), FDA, NFPA and Chemo ASTM 6978
ISO 9002 Certified Manufacturing
Quality sampled in accordance with MIL STD 105E
*Brand new state-of-the-art manufacturing plant with computer-controlled market leading technology |  | 
Defect | Inspection Level | AQL
Pinholes (FDA 1000 ml watertight test) | G1 | 1.5
Visual Defects (Major) | G1 | 2.5
Visual Defects (Minor) | G1 | 4.0
Dimensions | S-2 | 4.0